|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Mesh cloth | DONGGUAN LU YU SHOES MATERIAL CO..LTD | LY-1366(100%Recycled polyester) | Complied with Glow-Wire test at 550 °C | IEC/EN 62368-1 | Tested with appliance |
| 实物图片D:\Documents\WeChat Files\wxid_7n4vrfqmlj6p21\FileStorage\Temp\f923dd2fbe36041e4439c865575f422.jpg | | | | | |
| Mesh cloth | DONGGUAN LU YU SHOES MATERIAL CO..LTD | LY-24234(100%Recycled polyester) | Complied with Glow-Wire test at 550 °C | IEC/EN 62368-1 | Tested with appliance |
| 实物图片D:\Documents\WeChat Files\wxid_7n4vrfqmlj6p21\FileStorage\Temp\1721117748732.png | | | | | |
| Mesh cloth | DONGGUAN LU YU SHOES MATERIAL CO..LTD | LY-24234-1(100%Recycled polyester) | Complied with Glow-Wire test at 550 °C | IEC/EN 62368-1 | Tested with appliance |
| 实物图片 | | | | | |
| Mesh cloth | DONGGUAN LU YU SHOES MATERIAL CO..LTD | LY-W3117(100%Recycled polyester) | Complied with Glow-Wire test at 550 °C | IEC/EN 62368-1 | Tested with appliance |
| 实物图片 | | | | | |
| Mesh cloth | DONGGUAN LU YU SHOES MATERIAL CO..LTD | LY-S230518 | Complied with Glow-Wire test at 550 °C | IEC/EN 62368-1 | Tested with appliance |
| 实物图片 | | | | | |
| Mesh cloth | DONGGUAN LU YU SHOES MATERIAL CO..LTD | LY-S230522 | Complied with Glow-Wire test at 550 °C | IEC/EN 62368-1 | Tested with appliance |
| 实物图片 | | | | | |
| Mesh cloth | DONGGUAN LU YU SHOES MATERIAL CO..LTD | LY-5158 | Complied with Glow-Wire test at 550 °C | IEC/EN 62368-1 | Tested with appliance |
| 实物图片 | | | | | |
| Mesh cloth | DONGGUAN LU YU SHOES MATERIAL CO..LTD | LY-JH5 | Complied with Glow-Wire test at 550 °C | IEC/EN 62368-1 | Tested with appliance |
| 实物图片 | | | | | |